PRODUCT DESCRIPTIONS AND SPECIFICATIONS

Site:	CALGA				Product:	FACTORY DOUBLE WASHED SAND

General characteristics:

Sharp, free flowing sand generally off-white in colour. The production process of double washing and screening ensure clean sand is produced of high silica content.

Product specifications:

The product shall conform to the target specification as tabled below:

| Particle Size Distribution (AS 1141.11) | Target Grading Envelope % Passing |
| --- | --- |
| 4.75mm | 95 - 100 |
| 2.36mm | 95 – 100 |
| 1.18mm | 90 - 100 |
| 600 µm | 75 - 95 |
| 300µm | 30 - 50 |
| 150µm | 0 - 10 |
| 75µm | 0 - 2 |
| Clay & Fine Silt (AS1141.33) | 0 – 8 % |
| Moisture Content | 0 – 10 % |

Applications:

Used widely for the manufacture of pre-cast concrete products and, also with-in specialized

manufacturing processes. It is ideally suited to those applications calling for a clean, shell

free, colour consistent fine aggregate.